Fe掺杂SrSnO3陶瓷的制备及其特性的研究

李宏1,2

（1.淮北师范大学物理与电子信息学院，安徽 淮北 235000；2.上海交通大学物理系，上海 200240）

［摘要］以SrCO3、SnO2和Fe3O4为原料，采用传统固相反应法制备了Fe掺杂SrSnO3陶瓷，并借助XRD和SEM，研究了SrFexSn1-xO3的相结构、形貌及Fe掺杂量对其电性能的影响.XRD图谱表明：未经烧结的样品是混合物，随着烧结次数的增加，样品的收缩增大，成品纯度变高，XRD杂峰减少.Fe掺杂SrSnO3陶瓷中随着Fe含量从0增加到1，烧结温度逐渐降低，从1480 ℃下降到1200 ℃，其晶格常数从0 .806 9 nm下降到0 .773 6 nm，晶体结构没有发生明显改变.SEM图片显示，靶材晶粒随着掺杂量的增加逐渐增大，由2 .09 μm增加到4 .93 μm.

[关键词] 固相反应法；粉末；靶材；XRD；SEM；晶格常数；掺杂

Preparation and Properties of Fe Doped SrSnO3 Ceramics

LI Hong1,2

(1.School of Physics and Electronic Information，Huaibei Normal University，Huaibei 235000，China；2.Department of Physics,Shanghai Jiao Tong University,Shanghai 200240,China)

Abstract：Using SrCO3，SnO2 and Fe3O4 as starting materials，SrSnO3 ceramics were prepared by conventional solid-state reaction method.The effects of phase structure，morphology and Fe -doping on the electric properties of SrFexSn1-xO3 ceramics were investigated by X-ray Diffraction (XRD) and Scanning Electron Microscopy (SEM).XRD patterns indicated that the sample without sintering was a mixture.With increasing the number of sintering，the contraction of the sample increased，the purity of the finished product became higher，XRD＇s impure peaks decreased.With the iron increasing from 0 to 1 in SrSnO3，the sintering temperature decreased from 1480 ℃ to 1200 ℃ gradually，the crystal lattice parameter from 0 .806 9 nm down to 0 .773 6 nm，the crystal structure of SrSnO3 did not change clearly.SEM images showed the crystal size of targets increased from about 2 .09 μm to 4 .93 μm with the iron-doping increaseing.

Key words：solid-state reaction method；powder；target；XRD；SEM；crystal lattice parameter；doping